Outline

Course on powder X-ray diffraction - materials charaCterization

by C. kappenstein

emeritus professor, university of poitiers

#### I – cristallography

1. – POINT LATTICES

1.1. - Crystal space lattice

1.1.1. - Definitions

1.1.2. - Lines and planes

1.1.3. - Set of planes - Miller indices

1.2. - Reciprocal lattice

1.2.1. - Diffraction condition

1.2.2. - Properties of the reciprocal lattice

1.3. - Applications of reciprocal lattice

1.3.1. - Miller indices (h k l)of a set of planes defined by two lines

1.3.2. - Indices u v w of a line defined by two planes

1.3.3. - Angle between two faces of a crystal

1.3.4. - Building the reciprocal lattice

1.3.5. - d-spacing determination

1.4. - Basis changes

2. – Crystallographic groups

2.1. - Crystal lattices

2.2 -. 14 Bravais lattices

2.3. - Space groups

2.3.1. - 7 one-dimensional space groups

2.3.2. - 17 two-dimensional space groups

2.3.3. - 230 three-dimensional space groups

II – X-ray diffraction

1. – Introduction

# 2. – INTERACTION between X-rays and matter

## 2.1. - Fundamental processes

### 2.1.1. – Photoelectric effect

### 2.1.2. – Compton scattering

### 2.1.3. – Fluorescence

### 2.1.4. – Thomson scattering

2.2. - Absorption of X-rays

2.3. - Thomson coherent diffusion

2.3.1. – Scattering by a single electron

2.3.2. – Scattering by an atom: atom scattering factor

# 3. - DIFFRACTION by a periodic lattice

## 3.1. - Diffraction condition

3.2. – Ewald’s sphere

3.3. – Bragg’s relation

3.4. - Structure Factor

3.5. – Systematic absences

3.6. - Lorentz-polarization Factor Lp

3.7. - Debye-Waller factor DW

3.8. - Multiplicity factor Mhkl

3.9. – General relation

3.10. – Peak width – Scherrer’s relation

III – Powder diffractometer

1. – Source of X-rays

1.1. – X-ray tube

## 1.2. – White radiation

1.3. – Characteristic lines

1.4. – Take-off angle

2. - DETECTION of x-rays

## 2.1. - Proportional scintillation detector

## 2.2. – Linear detector

## 2.3. – Counting statistics

## 2.4. – Standard deviation and intensity

## 2.5. – Stability of the X-ray source

3. – Sampling

## 3.1. – Sample preparation

## 3.2. – different sample holders

4. – size of the irradiated area

4.1. – Sample holder

4.2. – Determination of the length L

4.3. – Determination of the width l

4. - DIFFRACTOMETer

4.1. – Measurement circle

4.2. - Focalization circle

4.3. – Opening slits

5. - CORRECTIONS

5.1. – Zero correction

5.2. – Sample displacement

5.3. – Sample absorption

5.4. – Flatness correction

5.5. – Axial divergence

5.6. – Displacement determination

6. – peak profile ANALYSIS

7. – DATA TREATMENT